## Slide 1
Since 1959
Atom dynamics in nanoparticles
T. Pradeep
Institute Professor, IIT Madras
https://pradeepresearch.org/
pradeep@iitm.ac.in
Co-founder
InnoNano Research Pvt. Ltd.
InnoDI Water Technologies Pvt. Ltd.
VayuJAL Technologies Pvt. Ltd.
Aqueasy Innovations Pvt. Ltd.
Hydromaterials Pvt. Ltd.
EyeNetAqua Pvt. Ltd.
Deepspectrum Analytics Pvt. Ltd.
Associate Editor
Professor-in-charge
International Centre for Clean Water
FS-CHM 2022 IISER Thiruvananthapuram, April 8-10, 2022
Lecture 9
Materials
Water
Devices

## Slide 2
Also the pioneering work of R. W. Murray, Robert L. Whetten, Uzi Landman, Tatuya Tsukuda, Yuichi Negishi, Hannu Hakkinen,
Rongchao Jin, Nanfeng Zheng, Terry Bigioni, Osman Bakr, Kornberg, Jianping Xie, C. M. Aikens, Thomas Buergi, Amala Dass, Ackerson, De-en Jiang, …. A. W. Castleman Jr., H. Schmidbauer, …
Citations: >1100

## Slide 3
Au25, Ag25, Ag29

## Slide 4
Au25L18-
Molecular formula, Molecular weight
Au38SR24
Au102SR44

## Slide 5
They make high quality crystals

## Slide 6
Geometric and electronic shells
Molecular structure
Gana Natarajan

## Slide 7
Molecules and their properties

## Slide 8
m/z
Ag29(BDT)123-
Ag25(DMBT)18-
Au25(PET)18-
HRMS of Au25(PET)18-

## Slide 10
Ananthu Mahendranath et al. Chem.Comm.2021

## Slide 11
Nanfeng Zheng et al. Nature Communications, 2013
Terry Bigioni et al. Nature 2013
Ag44

## Slide 12
Reactions on clusters
Reactions between clusters
Molecular reactions

## Slide 13
Inter-cluster reactions
A + B  C + D

## Slide 14
Au25(FTP)18 + Ag44(FTP)30 Au25-xAgx(FTP)18

## Slide 16
Energies for the substitution reaction of (A) Au in Ag44(SR)30, (B) Ag in Au25(SR)18 and (C) the overall reaction energies (in eV) as a function of their positions in product clusters, AuxAg44-x(SR)30 and Au25-xAgx(SR)18 for x=1

## Slide 17
Ag25-Au25 experiments
K. R. Krishnadas et al. Nature Commun. 2016

## Slide 18
Reaction between Au25(PET)18 and Ag25(DMBT)18
DMBT
PET

## Slide 19
Ag25(DMBT)18
Au25(PET)18
[Ag25(DMBT)18+Au25(PET)18]2-
[Ag25(DMBT)18+Au25(PET)18]2-
DMBT
PET

## Slide 20
within 2 min
within 5 min
Ag25(DMBT)18:Au25(PET)18
0.3:1.0
Evolution of alloy clusters from the dianionic adduct,
[Ag25Au25(DMBT)18(PET)18]2-

## Slide 21
Optimized structure of [Ag25Au25(DMBT)18(PET)18]2-

## Slide 23
How do we comprehend this?

## Slide 25
Gana Natarajan et. al. JPC C 2015

## Slide 26
Aspicules

## Slide 27
(D1-3,D2-3)-di(2-phenylethylthiolato),16(methylthiolato)-auro-25 aspicule(1-)
(D1-3,D2-3)-(PET)2,(SMe)16-auro-25 aspicule(1-)

## Slide 28
x
z´
y´
y
x´
3
5
3
1
4
2
1
3
4
4
4
1
1
5
4
5
5
2
2
1
2
4
3
2
5
1
2
3
5
z
3
Au
S
4
1
2
3
5
6
7
i
8
9
10
11
12
Ligand Exchange & Alloy cluster
Au24Pd(SR1)10(SR2)8 isomer 1 (cis)
1, 5-(SBB)10, 3-(SC6H12)8
(i, 1, 2, x2)-palladoauro-25 asp (-1)
x
y
z

## Slide 29
R-(SMe)44-auro-102 aspicule(0) and L-(SMe)44-auro-102 aspicule(0)

## Slide 31
M. Neumaier, A. Baksi, et. al., JACS 2021
Manfred Kappes, KIT

## Slide 32
CID data of [Au25Ag25]2-

## Slide 33
Kinetics of the exchange (monitored on the Ag25 side)

## Slide 34
Expanding reactions

## Slide 36
Interparticle Reactions Forming Product Co-Crystals

## Slide 37
Ag40 and Ag46 with the same shell
M. Bodiuzzaman, et. al. Angew. Chem. Int. Ed. 2018
Co-crystals

## Slide 38
Atom transfer dynamics
They are indeed molecules!

## Slide 40
ESI MS of A) 107Ag25(DMBT)18 and B)109Ag25(DMBT)18. Insets shows the respective isotope patterns.

## Slide 42
Papri Chakraborty, et. al. Science Advances 2019

## Slide 44
Can clusters react with nanoparticles?

## Slide 45
Paulami Bose et al. Nanoscale 2020

## Slide 48
Colloidal crystal
1 µm
100 µm
Interparticle reactions routed crystallization of nanoparticles
A
B
C
C
Paulami Bose et al. Unpublished

## Slide 49
2019
Outlook

## Slide 50
Molecules and their properties
Molecular formula
Molecular weight
Molecular structure
Molecular absorption and emission
Molecular reactions
Molecular assembly
Molecular co-crystals
------
Phases - phase transitions
Physical properties
Electrical, magnetic
Mechanical properties
Electrochemical properties
Future?

## Slide 52
Thank you all
Department of Science and Technology
Collaborators: Tatsuya Tsukuda, Keisaku Kimura, Yuichi Negishi, Uzi Landman, Rob Whetten, Hannu Hakkinen, Robin Ras, Manfred Kappes, Horst Hahn, Tomas Base, Shiv Khanna, Umesh Waghmare, Chandrabhas Narayana, Giridhar U. Kulkarni, Reji Philip, Vivek Polshettiwar, R. Mukhopadhay