## Slide 1
Since 1959
Complexity in the Chemistry of Atomically Precise Clusters
T. Pradeep
Institute Professor, IIT Madras
https://pradeepresearch.org/
pradeep@iitm.ac.in
Co-founder
InnoNano Research Pvt. Ltd.
InnoDI Water Technologies Pvt. Ltd.
VayuJAL Technologies Pvt. Ltd.
Aqueasy Innovations Pvt. Ltd.
Hydromaterials Pvt. Ltd.
EyeNetAqua Pvt. Ltd.
Deepspectrum Analytics Pvt. Ltd.
Associate Editor
Professor-in-charge
International Centre for Clean Water
Indo-German mini-workshop-2022, Complex Chemical Systems (IGW-CCS-2022), IIT Madras, October 5, 2022

## Slide 2
Au25, Ag25, Ag29

## Slide 3
Also the pioneering work of R. W. Murray, Robert L. Whetten, Uzi Landman, Tatuya Tsukuda, Yuichi Negishi, Hannu Hakkinen,
Rongchao Jin, Nanfeng Zheng, Terry Bigioni, Osman Bakr, Kornberg, Jianping Xie, C. M. Aikens, Thomas Buergi, Amala Dass, Ackerson, De-en Jiang, …. A. W. Castleman Jr., H. Schmidbauer, …. Robin Ras, Olli Ikkala
Citations: >1200
…Manfred Kappes, Horst Hahn

## Slide 4
Au25L18-
Molecular formula, Molecular weight
Au38SR24
Au102SR44

## Slide 5
m/z
Ag29(BDT)123-
Ag25(DMBT)18-
Au25(PET)18-
HRMS of Au25(PET)18-

## Slide 6
They make high quality crystals

## Slide 7
Geometric and electronic shells
Molecular structure
Gana Natarajan

## Slide 8
Molecules and their properties

## Slide 10
Ananthu Mahendranath et al. Chem.Comm.2021

## Slide 11
Nanfeng Zheng et al. Nature Communications, 2013
Terry Bigioni et al. Nature 2013
Ag44

## Slide 12
Reactions on clusters
Reactions between clusters
Molecular reactions

## Slide 13
Inter-cluster reactions
A + B  C + D

## Slide 14
Au25(FTP)18 + Ag44(FTP)30 Au25-xAgx(FTP)18

## Slide 16
Energies for the substitution reaction of (A) Au in Ag44(SR)30, (B) Ag in Au25(SR)18 and (C) the overall reaction energies (in eV) as a function of their positions in product clusters, AuxAg44-x(SR)30 and Au25-xAgx(SR)18 for x=1

## Slide 17
Ag25-Au25 experiments
K. R. Krishnadas et al. Nature Commun. 2016

## Slide 18
Reaction between Au25(PET)18 and Ag25(DMBT)18
DMBT
PET

## Slide 19
Ag25(DMBT)18
Au25(PET)18
[Ag25(DMBT)18+Au25(PET)18]2-
[Ag25(DMBT)18+Au25(PET)18]2-
DMBT
PET

## Slide 20
within 2 min
within 5 min
Ag25(DMBT)18:Au25(PET)18
0.3:1.0
Evolution of alloy clusters from the dianionic adduct,
[Ag25Au25(DMBT)18(PET)18]2-

## Slide 21
Optimized structure of [Ag25Au25(DMBT)18(PET)18]2-

## Slide 23
How do we comprehend this?

## Slide 25
Gana Natarajan et. al. JPC C 2015

## Slide 26
Aspicules

## Slide 27
(D1-3,D2-3)-di(2-phenylethylthiolato),16(methylthiolato)-auro-25 aspicule(1-)
(D1-3,D2-3)-(PET)2,(SMe)16-auro-25 aspicule(1-)

## Slide 28
x
z´
y´
y
x´
3
5
3
1
4
2
1
3
4
4
4
1
1
5
4
5
5
2
2
1
2
4
3
2
5
1
2
3
5
z
3
Au
S
4
1
2
3
5
6
7
i
8
9
10
11
12
Ligand Exchange & Alloy cluster
Au24Pd(SR1)10(SR2)8 isomer 1 (cis)
1, 5-(SBB)10, 3-(SC6H12)8
(i, 1, 2, x2)-palladoauro-25 asp (-1)
x
y
z

## Slide 29
R-(SMe)44-auro-102 aspicule(0) and L-(SMe)44-auro-102 aspicule(0)

## Slide 31
M. Neumaier, A. Baksi, et. al., JACS 2021
Manfred Kappes, KIT

## Slide 32
CID data of [Au25Ag25]2-

## Slide 33
Kinetics of the exchange (monitored on the Ag25 side)

## Slide 34
Expanding reactions

## Slide 36
Interparticle reactions forming product co-crystals

## Slide 37
Ag40 and Ag46 with the same shell
M. Bodiuzzaman, et. al. Angew. Chem. Int. Ed. 2018
Co-crystals

## Slide 38
Atom transfer dynamics
They are indeed molecules!

## Slide 40
ESI MS of A) 107Ag25(DMBT)18 and B)109Ag25(DMBT)18. Insets shows the respective isotope patterns.

## Slide 42
Papri Chakraborty, et. al. Science Advances 2019

## Slide 44
Can clusters react with nanoparticles?

## Slide 45
Paulami Bose et al. Nanoscale 2020

## Slide 47
Colloidal crystal
A
B
C
C
C
Crystallization of AgAu NP

## Slide 48
Bulk Au― Ag NC reaction

## Slide 49
Characterization of reaction products

## Slide 50
Supramolecular chemistry
Papri Chakraborty, et,. al. ACS Nano 2018
Expanding chemistry

## Slide 51
Figure 1. A) (a) Full range ESI MS, (b) experimental and calculated isotope patterns and (c) DFT optimized structure of [Ag29(BDT)12]3- cluster. B) (a) ESI MS of [Ag29(BDT)12(C60)n]3- (n=1-4) complexes, (b) experimental and calculated isotope patterns of [Ag29(BDT)12(C60)4]3- and (c) schematic of the possible structure of [Ag29(BDT)12(C60)4]3-.

## Slide 52
Isomerism in supramolcular adducts
Abhijit Nag, et al. JACS 2018

## Slide 53
X3-
X∩CD13-
X∩CD23-
X∩CD33-
Ag29BDT12 = X
β-cyclodextrin = CD
CD-
m/z
X∩CD63-
X∩CD53-
X∩CD43-
X∩CD13-
Calculated
Experimental
A)
a)
b)
m/z
X∩CD13-

## Slide 54
Drift time (ms)
Isomer 1
Isomer 2
X∩CD33-
628.0 Å2
613.0 Å2
Isomer 1
Isomer 2
X∩CD23-
540.0 Å2
526.0 Å2
X∩CD13-
438.0 Å2
Drift time (ms)
X∩CD63-
903.0 Å2
X∩CD53-
812.0 Å2
Isomer 1
Isomer 2
X∩CD43-
724.0 Å2
705.0 Å2
a)
b)
c)
d)
e)
f)

## Slide 55
a)
b)
c)
A)
B)
a)
i)
ii)
b)
i)
c)
i)
ii)
1
2
3/5
4
5/3
6
1
2
1
6
1
2
3
1
2
6
1
2
3
6
1
1
2
4
6
C-Ag29(BDT)12∩CD2
T-Ag29(BDT)12∩CD2
C-Ag29(BDT)12∩CD3
T-Ag29(BDT)12∩CD3
C-Ag29(BDT)12∩CD4
T-Ag29(BDT)12∩CD4
Cis = C
Trans = T
ii)

## Slide 56
Assemblies and superstructures

## Slide 57
Nanoclusters in colloidal assemblies
Nonappa et al., Angew. Chem. Int. Ed. 2016, 55, 16035–16038.
Som, A. et al., Adv. Mater. 2016, 28, 2827–2833

## Slide 58
Atomically precise nanocluster assemblies encapsulating plasmonic gold nanorods
Chakraborty, A. et al., Angew. Chem. Int. Ed. 2018, 57, 6522–6526.

## Slide 59
2019
Outlook

## Slide 60
Jana et. al, Inorganic Chemistry (2022)
Carborane-thiol protected propeller-shaped photoresponsive silver nanomolecule
With Tomas Base

## Slide 61
Characterization of Ag21

## Slide 62
Structural details of Ag21

## Slide 63
Molecules and their properties
Molecular formula
Molecular weight
Molecular structure
Molecular absorption and emission
Molecular reactions
Molecular assembly
Molecular co-crystals
------
Phases - phase transitions
Physical properties
Electrical, magnetic
Mechanical properties
Electrochemical properties
Future?

## Slide 64
Nonappa
Robin Ras
Mauri Kostiainen
Collaborators
Manfred Kappes
Olli Ikkala
Tatsuya Tsukuda, Keisaku Kimura, Yuichi Negishi, Uzi Landman, Hannu Hakkinen, Rob Whetten, Tomas Base
Horst Hahn

## Slide 68
Thank you all
Department of Science and Technology
Collaborators: Tatsuya Tsukuda, Keisaku Kimura, Yuichi Negishi, Uzi Landman, Rob Whetten, Hannu Hakkinen, Robin Ras, Manfred Kappes, Horst Hahn, Tomas Base, Shiv Khanna, Umesh Waghmare, Chandrabhas Narayana, Giridhar U. Kulkarni, Reji Philip, Vivek Polshettiwar, R. Mukhopadhay