## Slide 1
Since 1959
Complexity in the Chemistry of Atomically Precise Clusters
T. Pradeep
Institute Professor, IIT Madras
https://pradeepresearch.org/
pradeep@iitm.ac.in
Co-founder
InnoNano Research Pvt. Ltd.
InnoDI Water Technologies Pvt. Ltd.
VayuJAL Technologies Pvt. Ltd.
Aqueasy Innovations Pvt. Ltd.
Hydromaterials Pvt. Ltd.
EyeNetAqua Pvt. Ltd.
Deepspectrum Analytics Pvt. Ltd.
Associate Editor
Professor-in-charge
International Centre for Clean Water
AsiaNANO 2022 Asian Conference on Nanoscience & Nanotechnology, Busan, November 9-11, 2022
Jeong-Woo Choi
Chairperson of AsiaNANO 2022
And colleagues

## Slide 2
Au25, Ag25, Ag29

## Slide 3
Also the pioneering work of R. W. Murray, Robert L. Whetten, Uzi Landman, Tatuya Tsukuda, Yuichi Negishi, Hannu Hakkinen,
Rongchao Jin, Nanfeng Zheng, Terry Bigioni, Osman Bakr, Kornberg, Jianping Xie, C. M. Aikens, Thomas Buergi, Amala Dass, Ackerson, De-en Jiang, …. A. W. Castleman Jr., H. Schmidbauer, …. Robin Ras, Olli Ikkala
Citations: >1200
…Manfred Kappes, Horst Hahn

## Slide 4
Au25L18-
Molecular formula, Molecular weight
Au38SR24
Au102SR44

## Slide 5
m/z
Ag29(BDT)123-
Ag25(DMBT)18-
Au25(PET)18-
HRMS of Au25(PET)18-

## Slide 6
They make high quality crystals

## Slide 7
Geometric and electronic shells
Molecular structure
Gana Natarajan

## Slide 8
Molecules and their properties

## Slide 9
Nanfeng Zheng et al. Nature Communications, 2013
Terry Bigioni et al. Nature 2013
Ag44

## Slide 10
Reactions on clusters
Reactions between clusters
Molecular reactions

## Slide 11
Inter-cluster reactions
A + B  C + D

## Slide 12
Au25(FTP)18 + Ag44(FTP)30 Au25-xAgx(FTP)18

## Slide 14
Energies for the substitution reaction of (A) Au in Ag44(SR)30, (B) Ag in Au25(SR)18 and (C) the overall reaction energies (in eV) as a function of their positions in product clusters, AuxAg44-x(SR)30 and Au25-xAgx(SR)18 for x=1

## Slide 15
Ag25-Au25 experiments
K. R. Krishnadas et al. Nature Commun. 2016

## Slide 16
Reaction between Au25(PET)18 and Ag25(DMBT)18
DMBT
PET

## Slide 17
Ag25(DMBT)18
Au25(PET)18
[Ag25(DMBT)18+Au25(PET)18]2-
[Ag25(DMBT)18+Au25(PET)18]2-
DMBT
PET

## Slide 18
within 2 min
within 5 min
Ag25(DMBT)18:Au25(PET)18
0.3:1.0
Evolution of alloy clusters from the dianionic adduct,
[Ag25Au25(DMBT)18(PET)18]2-

## Slide 19
Optimized structure of [Ag25Au25(DMBT)18(PET)18]2-

## Slide 21
How do we comprehend this?

## Slide 23
Gana Natarajan et. al. JPC C 2015

## Slide 24
Aspicules

## Slide 25
(D1-3,D2-3)-di(2-phenylethylthiolato),16(methylthiolato)-auro-25 aspicule(1-)
(D1-3,D2-3)-(PET)2,(SMe)16-auro-25 aspicule(1-)

## Slide 26
x
z´
y´
y
x´
3
5
3
1
4
2
1
3
4
4
4
1
1
5
4
5
5
2
2
1
2
4
3
2
5
1
2
3
5
z
3
Au
S
4
1
2
3
5
6
7
i
8
9
10
11
12
Ligand Exchange & Alloy cluster
Au24Pd(SR1)10(SR2)8 isomer 1 (cis)
1, 5-(SBB)10, 3-(SC6H12)8
(i, 1, 2, x2)-palladoauro-25 asp (-1)
x
y
z

## Slide 27
R-(SMe)44-auro-102 aspicule(0) and L-(SMe)44-auro-102 aspicule(0)

## Slide 29
M. Neumaier, A. Baksi, et. al., JACS 2021
Manfred Kappes, KIT

## Slide 30
CID data of [Au25Ag25]2-

## Slide 31
Kinetics of the exchange (monitored on the Ag25 side)

## Slide 32
Expanding reactions

## Slide 34
Interparticle reactions forming product co-crystals

## Slide 35
Ag40 and Ag46 with the same shell
M. Bodiuzzaman, et. al. Angew. Chem. Int. Ed. 2018
Co-crystals

## Slide 36
Atom transfer dynamics
They are indeed molecules!

## Slide 38
ESI MS of A) 107Ag25(DMBT)18 and B)109Ag25(DMBT)18. Insets shows the respective isotope patterns.

## Slide 40
Papri Chakraborty, et. al. Science Advances 2019

## Slide 42
Can clusters react with nanoparticles?

## Slide 43
Paulami Bose et al. Nanoscale 2020

## Slide 45
Colloidal crystal
A
B
C
C
C
Crystallization of AgAu NP

## Slide 46
Bulk Au― Ag NC reaction

## Slide 47
Characterization of reaction products

## Slide 48
Supramolecular chemistry
Papri Chakraborty, et,. al. ACS Nano 2018
Expanding chemistry

## Slide 49
Figure 1. A) (a) Full range ESI MS, (b) experimental and calculated isotope patterns and (c) DFT optimized structure of [Ag29(BDT)12]3- cluster. B) (a) ESI MS of [Ag29(BDT)12(C60)n]3- (n=1-4) complexes, (b) experimental and calculated isotope patterns of [Ag29(BDT)12(C60)4]3- and (c) schematic of the possible structure of [Ag29(BDT)12(C60)4]3-.

## Slide 50
Isomerism in supramolcular adducts
Abhijit Nag, et al. JACS 2018

## Slide 51
X3-
X∩CD13-
X∩CD23-
X∩CD33-
Ag29BDT12 = X
β-cyclodextrin = CD
CD-
m/z
X∩CD63-
X∩CD53-
X∩CD43-
X∩CD13-
Calculated
Experimental
A)
a)
b)
m/z
X∩CD13-

## Slide 52
Drift time (ms)
Isomer 1
Isomer 2
X∩CD33-
628.0 Å2
613.0 Å2
Isomer 1
Isomer 2
X∩CD23-
540.0 Å2
526.0 Å2
X∩CD13-
438.0 Å2
Drift time (ms)
X∩CD63-
903.0 Å2
X∩CD53-
812.0 Å2
Isomer 1
Isomer 2
X∩CD43-
724.0 Å2
705.0 Å2
a)
b)
c)
d)
e)
f)

## Slide 53
a)
b)
c)
A)
B)
a)
i)
ii)
b)
i)
c)
i)
ii)
1
2
3/5
4
5/3
6
1
2
1
6
1
2
3
1
2
6
1
2
3
6
1
1
2
4
6
C-Ag29(BDT)12∩CD2
T-Ag29(BDT)12∩CD2
C-Ag29(BDT)12∩CD3
T-Ag29(BDT)12∩CD3
C-Ag29(BDT)12∩CD4
T-Ag29(BDT)12∩CD4
Cis = C
Trans = T
ii)

## Slide 54
Assemblies and superstructures

## Slide 55
Nanoclusters in colloidal assemblies
Nonappa et al., Angew. Chem. Int. Ed. 2016, 55, 16035–16038.
Som, A. et al., Adv. Mater. 2016, 28, 2827–2833

## Slide 56
Atomically precise nanocluster assemblies encapsulating plasmonic gold nanorods
Chakraborty, A. et al., Angew. Chem. Int. Ed. 2018, 57, 6522–6526.

## Slide 57
2019
Outlook

## Slide 58
Jana et. al, Inorganic Chemistry (2022)
Carborane-thiol protected propeller-shaped photoresponsive silver nanomolecule
With Tomas Base

## Slide 59
Characterization of Ag21

## Slide 60
Structural details of Ag21

## Slide 61
Molecules and their properties
Molecular formula
Molecular weight
Molecular structure
Molecular absorption and emission
Molecular reactions
Molecular assembly
Molecular co-crystals
------
Phases - phase transitions
Physical properties
Electrical, magnetic
Mechanical properties
Electrochemical properties
Future?

## Slide 62
Nonappa
Robin Ras
Mauri Kostiainen
Collaborators
Manfred Kappes
Olli Ikkala
Tatsuya Tsukuda, Keisaku Kimura, Yuichi Negishi, Uzi Landman, Hannu Hakkinen, Rob Whetten, Tomas Base
Horst Hahn

## Slide 66
Thank you all
Department of Science and Technology
Collaborators: Tatsuya Tsukuda, Keisaku Kimura, Yuichi Negishi, Uzi Landman, Rob Whetten, Hannu Hakkinen, Robin Ras, Manfred Kappes, Horst Hahn, Tomas Base, Shiv Khanna, Umesh Waghmare, Chandrabhas Narayana, Giridhar U. Kulkarni, Reji Philip, Vivek Polshettiwar, R. Mukhopadhay